Penetrant Process Planning Form

Document ID: QP-820-F1-PEN

Revision: A

Effective Date: September 1, 2025

- Penetrant Inspection Overview

| Product Name: | Penetrant Inspection |
| --- | --- |
| Specifications: | ASTM 1417-21 |
| Type: | TY I |
| Method: | Method A: Water Washable |
| Level: | Level 2 Sensitivity |
| Developer: | Form D: Non-Aqueous |
| Responsibility: | Level III |

- Scope:

This Process Plan defines the sequence of manufacturing/processing operations required to produce the above part in conformance with drawing, specification, and customer requirements.

- References:

- QM-001: Quality Manual

- QP-710: Inspection, Measure, and Test Equipment

- QP-820: Process Planning

- QP-850: Certificate of Conformance

- QP-8700: Control of Certified Materials

- QP-8800: Non-conforming Product

- QP-1010: Corrective Actions

- ASTM-1417-21: Standard Practice for Liquid Penetrant Testing

- QPL-AMS-2644: Penetrant Inspection Material

- Customer Requirements:

- Safety Precautions

  - Liquid penetrant materials are flammable and contain solvents that may cause skin and respiratory irritation. All penetrant processing shall be performed in accordance with this procedure and the Safety Data Sheet (SDS) maintained at the station.

  - Mandatory Personal Protective Equipment (PPE)

    - Chemical resistant nitrile gloves (change immediately if contaminated or torn)

    - Safety glasses with side shields per ANSI/ISEA 787.1

    - UV-A protective glasses or face shield block (blocks 99.9% UV-A) when under black light

    - Long sleeve Lab Coat

    - Respirator

  - Processing shall only be performed inside an approved booth

  - Eye wash station and safety shower shall be within 10 seconds of unobstructed travel distance and tested monthly.

  - Spill kits and class D fire extinguishers are located at each penetrant station.

  - Personnel shall be trained annually in chemical handling, spill response, and PPE use

  - Pregnant employees or those with known solvent sensitivity shall not perform penetrant operations

  - In the event of skin contact, immediately wash with soap and water. For eye contact, flush 15 minutes and seek medical attention.

  - Report all incidents to supervision immediately.

- Personnel

Only personnel currently certified to Level II or Level III in Liquid Penetrant Testing in accordance with NAS-410 are authorized to perform, interpret, and accept/reject parts during Type I, Method A fluorescent penetrant inspection. Certification status is verified daily through the S.M.A.R.T. system and records shall be maintained on file before any inspection begins. Vision examinations (near vision Jaeger 1 or equivalent at 12-16 and color perception) are current and recorded. All training, examination, and experience, and certification records are maintained by the Quality Department and available for customer or regulatory review.

- Risk Analysis

The fluorescent penetrant risk analysis (PEN-PFMEA) shall be recorded in QP-610-F1 Risk Register. All identified risks shall be handled in accordance with QP-610 Risk and Opportunity Management. No fluorescent penetrant inspection processing shall take place until all risks are identified and mitigated.

- Materials:

Materials utilized in the penetrant inspection process shall be listed on Table 1 and shall be certified. Material certifications shall be controlled per QP-8700 and recorded on QP-8700-F1 Material Storage. Materials shall not be utilized if they are expired (as applicable). Any expired materials found shall be handled per QP-8700. Only penetrants and cleaners listed on QPL-AMS-2644 are permitted unless customer PO specifically approves an alternate.

| Table 1: Materials |  |  |  |
| --- | --- | --- | --- |
| Material | Description | Specification | Manufacturer |
| Cloth | Cloth | AMS-3819 | Commercial |
| Solvent Cleaner | Acetone | ASTM D329 | Commercial |
| Penetrant | ZP-60D Level II Penetrant | QPL-AMS-2644 | Magnaflux |
| Developer | ZP-9F Non-Aqueous | QPL-AMS-2644 | Magnaflux |
| Water | DI water | ASTM D1193 | Commercial |
| Cotton Swabs | Cotton Swabs | NA | Commercial |

Note: 
1. All cans have an “in-date” and “open-date” label attached. No cans shall be used past the expiration date
2. Batch certifications shall be kept per QP-8700

- Equipment:

Equipment utilized in the penetrant process shall be listed on Table 2 and be calibrated (as applicable). Equipment calibrations shall be controlled per QP-710 and recorded on QP-710-F1 – Equipment Calibration Register. All penetrant inspection equipment shall not be utilized if the calibration is expired (as applicable). Any expired calibrations shall be handled per QP-710.

| Table 2: Equipment |  |  |
| --- | --- | --- |
| Equipment ID | Description | Calibrated? Yes or No |
| Pen-Timer-1 | Timer | Yes |
| Pen-Therm-1 | Thermometer | Yes |
| Pen-Pressure-Gauge | Pressure Gauge | Yes |
| Pen-Oven | Oven | Yes |
| Pen-Spray Gun | Spray Gun | No |
| Pen-UV Light | UV-Black Light | Yes |
| Pen-White Light | White Light | No |
| Pen-Light Meter | UV/White Light Meter | Yes |
| TAM Panel | TAM Panel | No |
| Pen-Measure | Indication Measuring Device | No |

- Process Flow (Sequence of Operations)

The TY I, Level II Sensitivity, Method A penetrant inspection shall follow the process flow in Table 3. Each operation step details the key characteristics of the process such as descriptions, materials required, material specifications, key process indicators, and equipment utilized. The penetrant inspection process is per ASTM-1417-21 and shall not deviate unless specified by customer PO and specifications.

| Table 3: Sequence of Operations and Key Characteristics |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Op. Number | Description | Material Required | Material Specifications | Key Process Indicator | Equipment |
| 01 | Clean | Acetone | ASTM D329 | Method: Wipe | - Powder Free Gloves - Cloth per AMS 3819 |
| 02 | Penetrant Dwell | Magnaflux: ZP-60D | QPL-AMS-2644 | Method A: Immersion Dwell Time: 10 Minutes minimum and 30 minutes maximum | - Thermometer - Timer |
| 03 | Penetrant Removal | DI Water | NA | Temperature: 50-100 F Pressure: 40 psi minimum | - Thermometer - Pressure Gauge - Spray Gun |
| 04 | Dry | NA | NA | Temperature: 139-169 F Drying Time: 10 minutes minimum | - Oven - Temperature - Timer |
| 05 | Developer | Magnaflux: ZP-9F | Non-Aqueous Developer | Dwell Time: 10 Minutes minimum, 1 hour maximum | - Timer |
| 06 | Examination | NA | NA | Method: 2 swabs per indication Eye Adaptation: 1 Minute minimum Black light: 1000 µW/cm² White light: 2 ftc maximum | - Black Light - White Light - Swabs - UV/White Light Meter |
| 07 | Post-Inspection Cleaning | Acetone | ASTM D329 | Method: Wipe | - Powder Free Gloves - Cloth per AMS 3819 |

- Work Instructions Procedure

  - BEFORE STARTING EVERY SHIFT

    - Put on full PPE

      - Chemical resistant nitrile gloves

      - Safety glasses with side shields

      - UV-blocking face shield or goggles

      - Long-sleeve Lab Coat

    - Check booth

      - Eye-wash and safety shower tested this month?

      - Spill Kit and Class D fire extinguisher in place

      - Booth door closed or black curtains drawn down

    - Daily Equipment Checks

      - Turn on UV-A black light for 10 minutes warm-up

      - Measure UV intensity at 15 inches from part area -> Must greater than 1000 µW/cm²

      - Measure visible (white) light in booth with light meter -> must be less than 2 foot-candles

      - Ensure all materials present are listed in Table 1, clearly labeled, and within expiration. No materials shall be used if the shelf-life is expired

      - Notify manager or supervisor immediately if 9.1.3.2 – 9.1.3.4 fails

  - Inspection Procedure

    - Receive the job

      - Get the traveler/router and the parts

      - Confirm the drawing or PO says “Type 1, Method A, Level 2” penetrant

      - Sign into the S.M.A.R.T. System. The system will verify your training credentials per NAS-410

      - Confirm your name, date, job number, part number, and heat-treat condition are listed.

    - Op. 1 Pre-clean the parts

      - Wipe parts clean with the acetone wipe

    - Op. 2 Apply Penetrant

      - Put parts in ZP-60D penetrant immersion tank

      - Start the time for a Dwell Time of 10 minutes 15 seconds minimum. The Dwell Time shall be 10 minutes minimum and not exceed a maximum of 30 minutes.

      - Record the dwell time and temperature of the penetrant application immersion tank

    - Op. 3 Penetrant Removal

      - Remove the parts from the application immersion tank and bring them to the rinse area

      - Grab the handheld spray gun and ensure the water pressure does not exceed 40 psi when spraying and verify the temperature is between 50- and 100-degrees F.

      - Spray the parts from a distance of 12 in. minimum. Do not over-wash the part. (Over-washing is indicated by a total lack of penetrant residue on the part)

      - Drain the part of excess water to prevent pooling in cavities, recesses, and pockets of the part.

    - Op. 4 Dry the parts

      - Air dry the parts until they are completely dry. The parts shall be completely dry and there shall be no indications of any remaining water.

      - Or. Place parts in the dryer oven.

      - Verify the oven is within class 2 calibration per AMS 2750 and set to 149 degrees F. The temperature shall be within 139-159 degrees F, and shall not exceed 160 degrees F.

      - Set the timer for 5 minutes. The parts shall be completely dry. There shall be no remnants of water anywhere on the part.

      - If the parts are not dry, set the timer for an additional 4 minutes. The parts shall not be dried for a total time of over 10 minutes maximum.

    - Op. 5 Develop the parts

      - Remove the parts from the oven and take to the viewing area

      - Spray the parts with the Magnaflux ZP-9F form d, Non-Aqueous Developer

      - Set the timer for 11 minutes and seconds. The development time shall be between 10 minutes minimum and 1 hour maximum.

      - Check the part for development, if the parts are fully developed begin the examination process in 9.2.7.

    - Op 6. Examination

      - Close the viewing area door or lower the black out curtain and darken the room.

      - Allow your eyes to adapt for a minimum of 1 minute. If you leave the darkened area for any reason, your eyes will need to re-adapt to the darkened area again for 1 minute minimum.

        - If you wear glasses, this must be recorded in accordance with NAS-410 and you must be wearing them.

        - Operators are not allowed to wear photochromic or permanently darkened lenses (sunglasses) when reviewing the parts.

      - Examine the parts for relevant indications per the customer’s acceptance criteria found on the applicable specification.

        - All areas of fluorescence shall be interpreted.

    - Indication Verification

      - Dampen a cotton swab with acetone.

      - Wipe the indication perpendicular to the length of the indication.

        - Operators are prohibited from swabbing the area more than twice.

      - Allow the area to dry

      - Spray developer on the area and set a time for 3 minutes and 15 seconds. The minimum redevelopment time shall be 3 minutes.

      - If the indication does not reappear, the indication may be considered false.

    - Indication Sizing

      - Evaluate the found indication by measuring the indication at its largest dimension with a measuring device against the customer’s acceptance criteria

      - Record any found indications or discontinuities that break the customer’s acceptance criteria

    - Op. 7 Post-Cleaning

      - Remove the parts from the viewing area

      - Wipe each part with acetone

      - Packaged the parts as they arrived for further processing

  - End of Job

      - Put all used rags in the red flammable waste bin

      - Return cans to shelf and write open-date on label if first use

      - Hang up PPE properly

      - File the completed inspection form for the job

- Final Inspection Release

All acceptance criteria of the Final Inspection Release Table shall be completed and in compliance with the appropriate acceptance criteria specification before any penetrant job per this process planning form can be issued a certificate of conformance (form QP-850-F1) for the customer. The acceptance criteria are derived from the specifications listed in Table 4. Any acceptance criteria that are not in compliance with the appropriate specification shall be handled per QP-8800 and a corrective action per QP-1010 shall be issued. When penetrant inspection is performed on the first piece of a new part number or after major process change, a First Article Inspection per AS9102 shall be completed prior to production release.

| Table 4: Final Inspection Release |  |  |
| --- | --- | --- |
| Acceptance Criteria Specification | Type | Acceptance Criteria |
| ASTM 1417-D21 | Equipment | All Equipment Calibration Check |
| ASTM 1417-D21 | Material | All Material Certifications within expiration |
| ASTM 1417-D21 | KPI | All Parameters Check |
| NAS-410 | Training | Training Certifications on file |
| ASTM 1417-D21 | TAM Panel | Daily TAM Panel Check on file |
| ASTM 1417-D21 | Periodic | Daily Penetrant Contamination Test |
| ASTM 1417-D21 | Periodic | 6-month Penetrant Brightness Test |
| ASTM 1417-D21 | Periodic | Weekly Water Content Test |
| ASTM 1417-D21 | Periodic | Daily System Performance Test |
| ASTM 1417-D21 | Periodic | Daily UV-A Lamp Intensity and Integrity Test |
| ASTM 1417-D21 | Periodic | Weekly Visible Light Intensity Test |
| ASTM 1417-D21 | Periodic | Daily Area Examination Cleanliness |
| ASTM 1417-D21 | Periodic | Quarterly Area Ambient Light Intensity Test |
| ASTM 1417-D21 | Periodic | Start of Each Shift Water Wash Pressure Check |
| ASTM 1417-D21 | Periodic | Start of Each Shift Water Temperature Check |
| Customer | XXX | XXX |

## Revision History

Approval Signatures

| Name | Title | Signature |
| --- | --- | --- |

Revision History

| Revision | Date | Description of Changes | Approved By |
| --- | --- | --- | --- |
| A | 8/15/2025 | Initial Draft |  |